MOSIS PARAMETRIC TEST RESULTS

RUN: T15D                                        VENDOR: AMI

TECHNOLOGY: SCN05                                FEATURE SIZE: 0.5 microns

INTRODUCTION: This report contains the lot average results obtained by MOSIS

from measurements of MOSIS test structures on each wafer of

this fabrication lot. SPICE parameters obtained from similar

measurements on a selected wafer are also attached.

COMMENTS: American Microsystems, Inc. C5N

TRANSISTOR PARAMETERS     W/L      N-CHANNEL P-CHANNEL  UNITS

MINIMUM                  3.0/0.6

Vth                                   0.80     -0.94  volts

SHORT                    20.0/0.6

Idss                                457      -248     uA/um

Vth                                   0.68     -0.92  volts

Vpt                                  10.0     -10.0   volts

WIDE                     20.0/0.6

Ids0                                < 2.5     < 2.5   pA/um

LARGE                    50/50

Vth                                   0.72     -0.96  volts

Vjbkd                                11.4     -11.7   volts

Ijlk                                <50.0     <50.0   pA

Gamma                                 0.47      0.59  V^0.5

K' (Uo*Cox/2)                         57.2     -18.8   uA/V^2

Low-field Mobility                   463.82    152.44  cm^2/V*s

COMMENTS: Poly bias varies with design technology. To account for mask and

etch bias use the appropriate value for the parameter XL in your

SPICE model card.

Design Technology                   XL

-----------------                   -------

SCN_SUBM (lambda=0.30)               0.00

AMI_C5                               0.00

SCN (lambda=0.35)                   -0.10

FOX TRANSISTORS           GATE      N+ACTIVE  P+ACTIVE  UNITS

Vth                      Poly        >15.0    <-15.0   volts

PROCESS PARAMETERS    N+ACTV P+ACTV   POLY  POLY2  MTL1   MTL2   MTL3  UNITS

Sheet Resistance      80.9  104.3   21.8   41.5   0.09   0.09   0.06  ohms/sq

Width Variation       -0.21  -0.22  -0.15  -0.07  0.05  -0.06  -0.07  microns

(measured - drawn)

Contact Resistance    67.0  150.5   15.8   27.5          0.82   0.64  ohms

Gate Oxide Thickness 140                                              angstrom

PROCESS PARAMETERS         POLY_HR  N\PLY      N_WELL   UNITS

Sheet Resistance          1077       838       835     ohms/sq

Width Variation                                        microns

(measured - drawn)

Contact Resistance                                     ohms

COMMENTS: N\POLY is N-well under polysilicon.

CAPACITANCE PARAMETERS N+ACTV P+ACTV   POLY  POLY2  M1  M2  M3  N_WELL  UNITS

Area (substrate)      426    733       88          31  16  10    40    aF/um^2

Area (N+active)                      2459          36  16  12          aF/um^2

Area (P+active)                      2375                              aF/um^2

Area (poly)                                 915    51  15   9          aF/um^2

Area (poly2)                                       47                  aF/um^2

Area (metal1)                                          31  13          aF/um^2

Area (metal2)                                              36          aF/um^2

Fringe (substrate)    328    263                   74  59  38          aF/um

Fringe (poly)                                      58  38  28          aF/um

Fringe (metal1)                                        47  32          aF/um

Fringe (metal2)                                            49          aF/um

Overlap (N+active)                    215                              aF/um

Overlap (P+active)                    234                              aF/um

CIRCUIT PARAMETERS                            UNITS

Inverters                     K

Vinv                        1.0       2.12  volts

Vinv                        1.5       2.38  volts

Vol (100 uA)                2.0       0.25  volts

Voh (100 uA)                2.0       4.74  volts

Vinv                        2.0       2.55  volts

Gain                        2.0     -22.79

Ring Oscillator Freq.

DIV256 (31-stg,5.0V)                106.46  MHz

Ring Oscillator Power

DIV256 (31-stg,5.0V)                  0.42  uW/MHz/gate

COMMENTS: SUBMICRON

T15D SPICE Level 3 PARAMETERS

*

* DATE: Jun 27/01

* LOT: T15D                  WAF: 02

* DIE: N_Area_Fring          DEV: N3740/10

* Temp= 27

.MODEL CMOSN NMOS (                                 LEVEL  = 3

+ TOX    = 1.4E-8          NSUB   = 1E17            GAMMA  = 0.5483559

+ PHI    = 0.7             VTO    = 0.7640855       DELTA  = 3.0541177

+ UO     = 662.6984452     ETA    = 3.162045E-6     THETA  = 0.1013999

+ KP     = 1.259355E-4     VMAX   = 1.442228E5      KAPPA  = 0.3

+ RSH    = 7.513418E-3     NFS    = 1E12            TPG    = 1

+ XJ     = 3E-7            LD     = 1E-13           WD     = 2.334779E-7

+ CGDO   = 2.15E-10        CGSO   = 2.15E-10        CGBO   = 1E-10

+ CJ     = 4.258447E-4     PB     = 0.9140376       MJ     = 0.435903

+ CJSW   = 3.147465E-10    MJSW   = 0.1977689       )

*

.MODEL CMOSP PMOS (                                 LEVEL  = 3

+ TOX    = 1.4E-8          NSUB   = 1E17            GAMMA  = 0.6243261

+ PHI    = 0.7             VTO    = -0.9444911      DELTA  = 0.1118368

+ UO     = 250             ETA    = 0               THETA  = 0.1633973

+ KP     = 3.924644E-5     VMAX   = 1E6             KAPPA  = 30.1015109

+ RSH    = 33.9672594      NFS    = 1E12            TPG    = -1

+ XJ     = 2E-7            LD     = 5E-13           WD     = 4.11531E-7

+ CGDO   = 2.34E-10        CGSO   = 2.34E-10        CGBO   = 1E-10

+ CJ     = 7.285722E-4     PB     = 0.96443         MJ     = 0.5

+ CJSW   = 2.955161E-10    MJSW   = 0.3184873       )

*

T15D SPICE BSIM3 VERSION 3.1 PARAMETERS

SPICE 3f5 Level 8, Star-HSPICE Level 49, UTMOST Level 8

* DATE: Jun 14/01

* LOT: T15D                  WAF: 02

* Temperature_parameters=Default

.MODEL CMOSN NMOS (                                LEVEL   = 49

+VERSION = 3.1            TNOM    = 27             TOX     = 1.4E-8

+XJ      = 1.5E-7         NCH     = 1.7E17         VTH0    = 0.6739432

+K1      = 0.8138857      K2      = -0.0762569     K3      = 23.316539

+K3B     = -7.6829409     W0      = 1E-8           NLX     = 1E-9

+DVT0W   = 0              DVT1W   = 0              DVT2W   = 0

+DVT0    = 3.3812941      DVT1    = 0.4195418      DVT2    = -0.0976246

+U0      = 455.8212463    UA      = 1.052138E-13   UB      = 1.60328E-18

+UC      = 1.871789E-11   VSAT    = 1.707997E5     A0      = 0.5973318

+AGS     = 0.1245402      B0      = 2.831408E-6    B1      = 5E-6

+KETA    = -2.751014E-3   A1      = 1.772392E-4    A2      = 0.3604111

+RDSW    = 1.297087E3     PRWG    = 0.0502651      PRWB    = 0.0351053

+WR      = 1              WINT    = 2.495013E-7    LINT    = 2.447934E-8

+XL      = 0              XW      = 0              DWG     = -1.882273E-8

+DWB     = 5.550376E-8    VOFF    = -3.376733E-4   NFACTOR = 1.0263478

+CIT     = 0              CDSC    = 2.4E-4         CDSCD   = 0

+CDSCB   = 0              ETA0    = 0.0014995      ETAB    = -1.245874E-3

+DSUB    = 0.1717116      PCLM    = 2.2954854      PDIBLC1 = -0.1582631

+PDIBLC2 = 2.890851E-3    PDIBLCB = -0.1267271     DROUT   = 0.3496078

+PSCBE1  = 5.629014E8     PSCBE2  = 5.268798E-5    PVAG    = 0

+DELTA   = 0.01           RSH     = 80.9           MOBMOD  = 1

+PRT     = 0              UTE     = -1.5           KT1     = -0.11

+KT1L    = 0              KT2     = 0.022          UA1     = 4.31E-9

+UB1     = -7.61E-18      UC1     = -5.6E-11       AT      = 3.3E4

+WL      = 0              WLN     = 1              WW      = 0

+WWN     = 1              WWL     = 0              LL      = 0

+LLN     = 1              LW      = 0              LWN     = 1

+LWL     = 0              CAPMOD  = 2              XPART   = 0.5

+CGDO    = 2.15E-10       CGSO    = 2.15E-10       CGBO    = 1E-9

+CJ      = 4.228884E-4    PB      = 0.99           MJ      = 0.449304

+CJSW    = 3.56272E-10    PBSW    = 0.1            MJSW    = 0.1213831

+CJSWG   = 1.64E-10       PBSWG   = 0.1            MJSWG   = 0.1213831

+CF      = 0              PVTH0   = 0.0601933      PRDSW   = 48.8936612

+PK2     = -0.0338264     WKETA   = -0.0213488     LKETA   = 5.133767E-3     )

*

.MODEL CMOSP PMOS (                                LEVEL   = 49

+VERSION = 3.1            TNOM    = 27             TOX     = 1.4E-8

+XJ      = 1.5E-7         NCH     = 1.7E17         VTH0    = -0.9365465

+K1      = 0.5526871      K2      = 9.463397E-3    K3      = 6.3646558

+K3B     = -0.5706084     W0      = 1E-8           NLX     = 1.900907E-8

+DVT0W   = 0              DVT1W   = 0              DVT2W   = 0

+DVT0    = 2.3523777      DVT1    = 0.5408808      DVT2    = -0.1254584

+U0      = 221.332531     UA      = 3.087011E-9    UB      = 1E-21

+UC      = -5.29755E-11   VSAT    = 1.859021E5     A0      = 0.8487879

+AGS     = 0.1434459      B0      = 1.097924E-6    B1      = 5E-6

+KETA    = -3.702499E-3   A1      = 0              A2      = 0.3

+RDSW    = 3E3            PRWG    = -0.046293      PRWB    = -0.0399508

+WR      = 1              WINT    = 2.942356E-7    LINT    = 4.298608E-8

+XL      = 0              XW      = 0              DWG     = -2.097829E-8

+DWB     = 2.184592E-8    VOFF    = -0.0678112     NFACTOR = 0.9055153

+CIT     = 0              CDSC    = 2.4E-4         CDSCD   = 0

+CDSCB   = 0              ETA0    = 6.960867E-3    ETAB    = -0.1077986

+DSUB    = 1              PCLM    = 2.183651       PDIBLC1 = 0.1051767

+PDIBLC2 = 4.351411E-3    PDIBLCB = -0.0435832     DROUT   = 0.2989224

+PSCBE1  = 1.268943E10    PSCBE2  = 1.235043E-9    PVAG    = 6.162441E-6

+DELTA   = 0.01           RSH     = 104.3          MOBMOD  = 1

+PRT     = 0              UTE     = -1.5           KT1     = -0.11

+KT1L    = 0              KT2     = 0.022          UA1     = 4.31E-9

+UB1     = -7.61E-18      UC1     = -5.6E-11       AT      = 3.3E4

+WL      = 0              WLN     = 1              WW      = 0

+WWN     = 1              WWL     = 0              LL      = 0

+LLN     = 1              LW      = 0              LWN     = 1

+LWL     = 0              CAPMOD  = 2              XPART   = 0.5

+CGDO    = 2.34E-10       CGSO    = 2.34E-10       CGBO    = 1E-9

+CJ      = 7.297461E-4    PB      = 0.9341338      MJ      = 0.4930142

+CJSW    = 2.993609E-10   PBSW    = 0.99           MJSW    = 0.3295232

+CJSWG   = 6.4E-11        PBSWG   = 0.99           MJSWG   = 0.3295232

+CF      = 0              PVTH0   = 5.98016E-3     PRDSW   = 14.8598424

+PK2     = 3.73981E-3     WKETA   = 8.349055E-3    LKETA   = -5.164353E-3    )

*